## Slide 1: TXM XANES Wizard part1 END
Apply the EJ filter and extract the AVG spectrum from the field of view (use filter + get bulk XANES).
In the main Wizard window, Misc  convert a folder to tiff. Save also the EJ filter in tif. (Save Images in TXM XanesWizard), then open it with ImageJ and convert it to 32bit (Image type 32bit), finally divide by 255 (Process  math  Divide) and save it as tif.
You can apply it to the stack.tif using again ImageJ (Import  Image Sequence and Process  Image Calculator  Multiply).
In ImageJ, Stacks  Plot Z profile. Select the image that corresponds to the maximum absorption. Here apply a threshold to separate material from white (empty) pixels: Image  Adjust  Threshold. When apply the selection choose the option “Set background to NaN”. And finally “reset” the stack. If you now extract the spectra with ImageJ you got the average just on the selected pixels by the EJ filter (pixels that contain material).
This is the output with the old Wizard.